## Slide 1
T2K Target and Beam Window Upgrades for 1.3 MW Operation
Chris Densham
(STFC Rutherford Appleton Laboratory)
On behalf of T2K Collaboration

## Slide 2
30 GeV PS
3 GeV PS
400 MeV LINAC
T2K neutrino facility
J-PARC, Tokai, Japan
T2K Target Station
295 km to Super-Kamiokande
Near detector
J-SNS
Beam dump

## Slide 3: T2K Operational performance

## Slide 4
Upgrade

## Slide 5: Secondary Beam-line & Target Station
Baffle
1st horn
Target
2nd horn
3rd horn
BEAM
Iron shield (2.2m)
Concrete Blocks
Helium Vessel
Target station
Beam window

## Slide 6: Target & Horn Assembly (latest version)

## Slide 7: Target & horn
p
Next target under construction
Next target under construction at RAL
Helium cooling flow lines
425 m/s

## Slide 8: CFX model heat inputs (MARS)

## Slide 9: Target upgrade requirements
The increase in design beam power from 0.751.3MW will increase the integrated heat load on the target (approx. 23kW  41kW).
Need to increase helium mass flow rate to keep outlet temperatures within range
Necessary to increase operating pressure to keep velocities and pressure drops within range.
  Increasing the pressure will increase the helium density and therefore heat transfer coefficient.
  Higher operating pressure has the advantage of reduced pressure drop.
  Running at higher pressure reduces the pressure drop and max velocity
  Compressor will be cheaper to purchase and operate (less power consumed).

## Slide 10: Simulations of target @ 1.3MW Increased beam power, flow rate & pressure
60g/s @ 5.9bar (5barG outlet) – 1.3MW beam power
Damaged graphite
Thermal conductivity 1/4
Helium flow lines

## Slide 11: Summary of cooling simulations
Flow rate [g/s] | Outlet Pressure [bar] | Beam power [kW] | Pressure drop [bar] | Max velocity [m/s] | Target core temp (damaged) [K] | Target core temp (new) [K]
32 | 0.9 | 750 | 0.73 | 560 | 1025 | 894.1
60 | 0.9 | 1300 | 1.93 | 870 |  | 960.3
60 | 2 | 1300 | 1.39 | 639 |  | 952.3
60 | 3 | 1300 | 1.09 | 501 |  | 951.1
60 | 5 | 1300 | 0.88 | 425 | 1182.6 | 951.9
Existing plant can deliver cooling power for 900 kW operation.
For 1.3MW beam @ 5bar and 60g/s, the velocity and pressure drop are comparable to 750 kW design.
Need to upgrade plant to operate at higher pressure.
Some target modifications needed to operate at higher pressure (e.g. window geometry, weld design, target pipes – bellows & isolators)
Target will run slightly hotter. Need high helium purity to avoid oxidation. (New target will withstand vacuum load to enable helium back fill)
NOTE: speed of sound in He ~1000m/s

## Slide 12: Target window re-optimisation for 5 bar operation
Parameterised re-optimisation of upstream window
Downstream window
Von-Mises stresses in existing target window at 5 bar
Optimised: 75 MPa -> 34 MPa
Plate thickness: 7 mm -> 10 mm
External radius = 7 mm
Internal radius = 25 mm

## Slide 13: Effect of pulsed beam on T2K target
Inertial ‘violin modes’ from worst-case off-centre beam spill
2-sigma beam offset
  0.5 mm amplitude
  6.8 MPa stress
Tolerant to worst case off-centre beam
Stress distribution after off-centre beam spill
Stress waves in graphite: on-centre beam spill
-8 MPa
5 µs beam spill
p
IG43 Compressive strength = 90 MPa
Tensile strength = 37 MPa

## Slide 14: Target supports and horn integration
Increasing horn current from 250 kA to 320 kA will increase vibrations
Target supports redesigned to prevent any movement
E.g. new ‘kinematic’ design feature
Angular adjustment is enabled whilst constraining position using spherical bushes

## Slide 15: Next target manufacture at RAL

## Slide 16: Graphite thermal conductivity degradation
400°C
600°C
800°C
Max core temperature ~900°C at 1.3 MW
(degraded graphite assumed)
Even a low radiation dose drastically reduces thermal conductivity
High temperatures reduce effect
Helium cooling lets target run hot
Also reduces swelling & changes to mechanical properties
As beam power increases, target failures are to be expected

## Slide 17: Target lifetime due to Oxidization
800C
700C
IG-430(U)
(purified)
Safety factor =2
2year
2year
Target center ~900C, but surface ~600C.
O2 contamination is kept as low as possible and will be improved by evacuating next target before back-filling with He
IG-43 (non-purified)

## Slide 18
T2K Target & horn in work cell

## Slide 19: T2K Target remote exchange system

## Slide 20: Remote Target Exchange System
Target exchanger and manipulator system. See pipe replacement at:
https://www.youtube.com/watch?v=VWGXz5QHFH4
Notes: Target exchange procedure
Target exchanger platform on gimbal/spring system, positioned by dual jacks, X and Z rails allow carriage cross over for target removal installation.
View of operators through RMA lead glass window.

## Slide 21: Leak at Helium Outlet Pipe & Remote Handling
304L
Stainless
Bent in cold process
Alumina ceramic
Diffusion bond
(Aluminum)
316L Stainless
Bellows
Failure of joint/ceramic from movement of stainless pipes (stress relieving) at 450 kW operation
Thermal fatigue failure of the diffusion bonded joint/ceramic
Remote Exchange in 2015
No leak since then

## Slide 22: Helium cooling pipe isolator R&D
Brazed ceramic with thermocouples attached undergoing a rapid cooling test
- Survived 10 thermal cycling tests – needs long term testing
Bolted isolator design with metal helicoflex seals
- Failed after c.10 thermal cycles
Existing ‘diffusion’ bonded joint made using aluminium wire
Works well at 485 kW but can it operate at 1.3 MW / multiple 160°C transients? Need to test!
We will know in a few months the best solution to use in next target – and whether it can survive multiple beam trips at 1.3 MW
Alternative solution: isolated heat exchanger – reduces temperatures

## Slide 23
Forced convection cooling blower
Noise reducing inlet baffles
Test ceramic isolator (welded into removable KF flange section for leak testing)
Test section tape heated (low thermal mass), enclosed in stainless box
Noise isolation box (rig suitable for 24h running)
Exhaust silencer/exhaust to external outlet
- Beam trips cause rapid cooling and repeated thermal cycling of ceramic isolators in helium cooling system
- Expected c.5000 beam trips / year
www.stfc.ac.uk
Ceramic Isolator Thermal Fatigue Test Rig
Beam Power [kW]
He in TS Vessel [℃]
He at Target inlet [℃]
He at Target outlet [℃]
Thermal transients from beam trips at 475 kW operation

## Slide 24
Ceramic Isolator Thermal Fatigue Test Rig
Thermal cycling testing now underway
Tape heater
PT100
KF50 for quick disconnect/leak testing
Interlock system
Eurotherm 3508 controller

## Slide 25: Target Summary
Existing target cooling plant suitable for up to 900 kW beam power
Operation at 1.3 MW appears feasible with incremental design changes to target
  windows, weld joints
Thermal cycling test program underway for ceramic isolators
Need new helium plant to operate at higher pressure
Target lifetime at 1.3 MW is not known

## Slide 26: Ti-6Al-4V Beam Window
Periodic thermal stress wave caused by the intense proton beam energy deposition
1.3 MW operation will cause radiation damage of ~2 DPA/ops-year
Significant irradiation hardening and loss of ductility has been reported with 0.3DPA (no higher DPA data exists)
No known data exists on high cycle fatigue (>103 cycles) of irradiated titanium alloys
Beam Power | PPP | Rep. cycle | POT / 100 days
470kW (achieved) | 2.4 x 1014 | 2.48 sec | （0.8 x 1021）
750kW (proposed) | 2.0 x 1014 | 1.3 sec | 1.3 x 1021
750kW [original plan] | 3.3 x 1014 | 2.1 sec | 1.3 x 1021
1.3 MW (proposed) | 3.2 x 1014 | 1.16 sec | 2.4 x 1021
designed
～1DPA/yr (MARS)
2mm gap
Ti-6Al-4V
(0.3mm-t)
~8M pulses/yr

## Slide 27: T2K beam window upgrade plans for - 1.3 MW
Pressure drop 0.06bar @ 1.1g/s
Max velocity 230 m/s
Strong recirculation zones driven by high speed jet
Helium flow lines
1.3 MW beam (steady state/CW simulation)

## Slide 28: Window thickness upgrade – for beam upgrade
Beam bunch structure can generate stress resonance within thickness of Ti alloy window material
Constructive interference at 0.36 mm (S.F.=1.5)
Destructive interference at 0.40 mm (S.F.=2.6)
0.40 mm selected for next beam window (just manufactured)
0.30 mm
~4.2 µs
581-598 ns
80 ns (3σ)
2.48 s → 1.16 s

## Slide 29: Window Remote Exchange (2017 summer)
The 1st window operated successfully up to 2.2x1021 POT
  Comparable to 1.3MW/ops-yr
Discoloration/deposit/damage of Ti-6Al-4V on TS vessel side visually identified
  Helium in TS vessel was humid, and the damage may be from radio-chemical reaction (accelerator vacuum side show less signatures)
  Need to improve helium circulation system to remove the humidity
We wish to perform PIE at JAEA’s hot-lab, but it will take time to clear radiation safety regulations and license problems at J-PARC
4m
30cm
After 2.2 x 1021 pot
~2DPA(NRT)

## Slide 30
R a D I A T E
Radiation Damage In Accelerator Target Environments
International collaboration to bring together the accelerator target and materials science communities
Next talk by T. Ishida
J-PARC MoU signing & workshop in 2017

## Slide 31: Summary
Plan to upgrade beam window thickness from 0.3 mm -> 0.4 mm to increase tolerance of beam window to thickness/bunch structure (and increase helium pressure)
Operation at 1.3 MW appears feasible for upgraded beam window
Radiation damage of materials is main question
→ Ishida-san talk