## Slide 1: Understanding control and modulation of color center defects
Vsevolod Ivanov
VTNSI & Physics
Dec 1, 2023

## Slide 2
From First-Principles to Quantum Detection
Defects/
Properties
Formation Conditions
Deterministic Creation
Quantum Detection
My Background

## Slide 3
Silicon Defects Team
Publications
https://arxiv.org/abs/2307.05759
https://arxiv.org/abs/2303.16283
https://arxiv.org/abs/2209.11412
Communications Materials 4, 22 (2023) [arxiv:2203.13781]
Nature Communications 14, 3321 (2023)[arxiv:2301.06654]
Phys. Rev. Applied 20, 014058 (2023) [arxiv:2302.05814]
Opt. Express 31 (5) 8352-8362 (2023)
[doi.org/10.1364/OE.482311]
Phys. Rev. B 106, 134107 (2022) [arxiv:2206.04824]
Work was done in collaboration with the groups of:
Liang Tan, LBNL (Theory)
Thomas Schenkel, LBNL (Experiment)
Boubacar Kante, UC Berkeley (Experiment)

## Slide 4: Outline
Introduction – Color Center Defects as Detectors
Color center defect types and detection strategies
Relevant defect properties we can compute
How Formation Conditions Impact Defect Properties
G-center structural isomers
Effect temperature and disorder on defect properties
Writing & erasing defects on demand
Defect Database & Future Work

## Slide 5: Outline
Introduction – Color Center Defects as Detectors
Color center defect types and detection strategies
Relevant defect properties we can compute
How Formation Conditions Impact Defect Properties
G-center structural isomers
Effect temperature and disorder on defect properties
Writing & erasing defects on demand
Defect Database & Future Work

## Slide 6
Detection Strategies for neutrons, neutrinos, and more!
Types of Color Centers
Vacancy – Host atom removed
Interstitial – element inserted into host gap
Substitutional – host atom replaced by element
Direct
Indirect
Formation
Low energy but low detection density
Works for dark defects but detection ambiguity
Don’t need prior defects but need ideal material

## Slide 7
Defect Properties
Zero-phonon line (ZPL): The primary energy (frequency) of emitted photons emitted by the defect
Application
Property
Single-photon sources

## Slide 8
Defect Properties
Zero-phonon line (ZPL): The primary energy (frequency) of emitted photons emitted by the defect
Application
Property
Linewidth: How broad the ZPL peak is (range of emitted frequencies)
Transition dipole moment: How well the transition couples with light
Single-photon sources

## Slide 9
Defect Properties
Zero-phonon line (ZPL): The primary energy (frequency) of emitted photons emitted by the defect
Application
Property
Linewidth: How broad the ZPL peak is (range of emitted frequencies)
Transition dipole moment: How well the transition couples with light
Single-photon sources
Energetics: Formation energy, ∆E for charge, isomers, local strain/disorder

## Slide 10: Outline
Introduction – Color Center Defects as Detectors
Color center defect types and detection strategies
Relevant defect properties we can compute
How Formation Conditions Impact Defect Properties
G-center structural isomers
Effect temperature and disorder on defect properties
Writing & erasing defects on demand
Defect Database & Future Work

## Slide 11
Defect structure & bonding determine properties
Phys. Rev. B 106, 134107 (2022) [arxiv.org/abs/2206.04824]
Optically Dark!
Optically Bright!

## Slide 12
Defect structure & bonding determine properties
Phys. Rev. B 106, 134107 (2022) [arxiv.org/abs/2206.04824]
Optically Dark!
Optically Bright!
20 meV
Direct

## Slide 13
Temperature control of defect formation
Opt. Express 31 (5) 8352-8362 (2023)

## Slide 14
Temperature control of defect formation
Opt. Express 31 (5) 8352-8362 (2023)

## Slide 15
Defects in the presence of disorder (vacancies/interstitials)
Phys. Rev. Applied 20, 014058 (2023)
Ion implantation step also damages the surrounding lattice → vacancies/interstitials
Disorder induces local strain, changing emitted photon energy.

## Slide 16
Defects in the presence of disorder (vacancies/interstitials)
Indirect
Directional detection using induced strain

## Slide 17
Writing and Erasing Defects
Introduce H into lattice → New Ci center observed! No G-centers!
https://arxiv.org/abs/2307.05759

## Slide 18
Writing and Erasing Defects
Forming gas + laser processing adds/removes H, turning defects ON/OFF
Ci-center (856 meV)
G-center (969 meV)
https://arxiv.org/abs/2307.05759

## Slide 19
Writing and Erasing Defects
Forming gas + laser processing adds/removes H, turning defects ON/OFF
OR
Ci - like
G - like

## Slide 20
Improve Indirect- and Formation-Based Detectors
Processing with forming gas → more variety of defects available in formation-based detection
Defect arrays → better positioning/ detection vs. single defects
add Forming Gas

## Slide 21
Defect emission enhancement in a nano-cavity
Nature Communications 14, 3321 (2023)

## Slide 22: Outline
Introduction – Color Center Defects as Detectors
Color center defect types and detection strategies
Relevant defect properties we can compute
How Formation Conditions Impact Defect Properties
G-center structural isomers
Effect temperature and disorder on defect properties
Writing & erasing defects on demand
Defect Database & Future Work

## Slide 23
Database of Quantum Defects
quantumdefects.com
~50,000 Multi-element defects →
Opportunities to explore elemental interactions & chemistry
Many new candidates for spin-photon interface (spin qubit) and bright single-photon sources!

## Slide 24
Database of Quantum Defects
quantumdefects.com
Phys. Rev. Applied 16, 064060x
arXiv:1902.10668 →

## Slide 25
Website
condensedmatters.com
Email
vivanov@vt.edu
Thank you!